[image: image1.png]



Vipac Engineers & Scientists Ltd
[image: image2.png]


Brandy Pines Pty Ltd

Insultec Coatings

Measurement of

Solar Heat Gain Properties

Rep No. 38630/M65

________________

Prepared by

Vipac Engineers & Scientists Ltd

March, 94

DOCUMENT CONTROL FORM

	INSULTEC COATINGS

MEASUREMENT OF SOLAR HEAT GAIN PROPERTIES

	FILE: SF630 




REPORT CODE: M65

PREPARED FOR:



PREPARED   BY

           

                                                                 

	Brandy Pines Pty Ltd



Vipac Engineers & Scientists Ltd.,

10 Maxwell Street



Victorian Technology Centre,

Ashburton, VIC 3147



275 Normanby Road,

AUSTRALIA




Port Melbourne, VIC. 3207







AUSTRALIA


Phone: (03) 885-9272



Phone: (03) 647- 9700

Fax:





Fax:      (03) 646- 4370




[image: image3.png][AUTHORES SR 1r/y
./dsfnﬁ/"w" Liees L2
'Dr// ah Fernando 6 Date:

REVIEWED BY: T ‘&w

D, Norman Broner

Date Issued Reason/Comments
Final
RevNo. Location
1 0 Vipac Metbaurnc
24 0 Brandy Pioss

Trsultes Coatings, Solar Feat Gain Properics





CONTENTS
DOCUMENT CONTROL FORM…………………………………………… 2

CONTENTS……………………………………………………………………3

1.0 INTRODUCTION…………………………………………………………3

2.0 METHODOLOGY…………………………………………………………4

3.0 RESULTS………………………………………………………………….4

FIGURES 

1.0    INTRODUCTION

Vipac Engineers and Scientists Ltd. was commissioned by Brandy Pines Pty Ltd. to measure the solar heat gain properties of Insultec Coatings to compare with those properties for commercially available roofing material. The absorbance of several samples of Insultec coatings and commercially available metal roofing materials were measured using a UV/IR Spectrophotometer. These measurements were then used to calculate the Solar Heat Gain (SHG), Solar Heat Gain Factor (SHGF), Shading Coefficient (SC), Overall Heat Transfer Coefficient (U-Value), and Maximum Surface Temperature, according to methods described in ASHRAE handbook 1993, Chapter 27.

The types of samples used for the test are;

Colorbond – Heritage Red

Colorbond – Off White

Colorbond – Mist Green

Galvanised Steel

Insultec – sample 1 - (0.01 mm thick coating

Insultec – sample 2 - (0.05 mm thick coating

Insultec – sample 3 - (0.01 mm thick coating

Insultec – sample 4 - (0.05 mm thick coating

Since only a flat sample was used for each test as per ASTM E903-82 the measured absorptance is diffused absorptance for normal incidence of the solar beam. The effect of Greco or Roma profile is not included in this procedure.   

2.0
Methodology
One test piece of dimension 13 mm x 50 mm was cut from each type of sheeting. The test piece was then placed in a GBC 916 UV-Visible Spectrophotometer and a PE-IR infra red spectrophotometer. The absolute diffused absorbance of each sample was measured for wavelengths 190 nm to 2500 nm (Figure 1) using Integrating Sphere attachment. The solar absorptance for the total solar spectrum was evaluated using the Air Mass 1 Spectrum (Figure 2)

The solar absorptance of the samples were calculated using the following formula in the wavelength range 190 nm – 2500nm.


% Absorptance
=
(a(() x S(()

x 100






   (S(()

where, S(() is the Air Mass 1 solar spectrum and a(() is the absorptance of the sample.

The above measurements were used with the typical properties of Galvanised steel to evaluate the Solar Heat Gain (SHG), Solar Heat Gain Factor (SHGF), Shading Coefficient (SC), Overall Heat Transfer Coefficient (U-Value), and Maximum Surface Temperature, using the methodology described in ASHRAE Fundamentals Handbook, Chapter 27

3.0 
RESULTS
The measured absorbance spectra were identical for the four Insultec Coated samples with different thicknesses. This implies that the solar heat transfer properties of the coatings do not depend on the coating thickness when the thickness is greater than (0.01mm. In the results shown in Figure 1 only one curve is used to represent all Insultec samples. 

The following standard conditions were assumed for the calculation of Solar Heat Gain Properties.

Solar Bean Intensity


782
W/m2.

Outside Temperature


  32
0C

Inside Temperature


  24
0C

Outside Wind Velocity


 3.3
m/s

Inside Wind Velocity


    0
m/s

Thermal Conductivity


50.5
W/m/K

Emissivity of Air


0.93


The results obtained are shown in Table 1.

Table 1: Solar Heat Transfer Properties of the Samples Tested

	Sample  
	Solar

Absorbance

%
	Overall Heat

Transfer

Coefficient

(U)

[W/m2/K}
	Maximum

Surface

Temp

[C]
	Solar

Heat

Gain

(W/m2)
	Solar

Heat

Gain

Factor

(SHGF)
	Shading

Co

efficient

(SC)

	Heritage Red
	80.2
	5.64
	49.9
	152.0
	0.19
	0.22

	Off White
	24.7
	5.42
	36.8
	52.4
	0.07
	0.08

	Mist Green
	54.2
	5.55
	44.2
	108.3
	0.14
	0.16

	Galv. Steel
	29.3
	5.44
	38.0
	61.6
	0.08
	0.09

	Insultec
	15.1
	5.38
	34.2
	32.7
	0.04
	0.05


The errors associated with the measurement and calculation of the above results are less than ( 3%.

Based on the above results Insultec Coatings have the best solar insulation properties. In terms of Solar Heat Gain, Insultec Coated sample is 38% better than the Off White – Colorbond sample and 47% better than the Galvanised Steel sample. The maximum surface temperature of the Insultec sample is only 2.2 0C higher than the ambient temperature whereas the corresponding temperature difference for Colorbond- Heritage Red sample is 17.9 0C. The Colorbond- Heritage Red sample show the worst solar insulation properties.

Based on the above test results and analysis it can be concluded that the Insultec Coatings provide a significant benefit in solar insulation when compared to the commonly used commercial metallic roofing materials.

Report Prepared

For

Brandy Pines Pty. Ltd.

By

VIPAC ENGINEERS & SCIENTISTS Ltd.

Figure 1: Absolute Diffused Absorption of the Samples Tested


[image: image4.wmf]0

0.5

1

1.5

0

200

400

600

800

1000

1200

1400

1600

1800

2000

2200

Absorptance

R e d

O f f  W h I t e

M i s t  G r e e n

G a l  S t e e l

I N S U L T E C







Wavelength (nm)

Figure 2: Solar Radiation Spectra (Air Mass)


[image: image5.wmf]0

0.2

0.4

0.6

0.8

1

1.2

1.4

1.6

1.8

2

200

400

600

800

1000

1200

1400

1600

1800

2000

2200

Wavelength (nm)

Solar Radiation (W/m)


_1099761000.xls
Chart2

		0		0		0		0		0

		50		50		50		50		50

		100		100		100		100		100

		150		150		150		150		150

		200		200		200		200		200

		250		250		250		250		250

		300		300		300		300		300

		350		350		350		350		350

		400		400		400		400		400

		450		450		450		450		450

		500		500		500		500		500

		550		550		550		550		550

		600		600		600		600		600

		650		650		650		650		650

		700		700		700		700		700

		750		750		750		750		750

		800		800		800		800		800

		850		850		850		850		850

		900		900		900		900		900

		950		950		950		950		950

		1000		1000		1000		1000		1000

		1050		1050		1050		1050		1050

		1100		1100		1100		1100		1100

		1150		1150		1150		1150		1150

		1200		1200		1200		1200		1200

		1250		1250		1250		1250		1250

		1300		1300		1300		1300		1300

		1350		1350		1350		1350		1350

		1400		1400		1400		1400		1400

		1450		1450		1450		1450		1450

		1500		1500		1500		1500		1500

		1550		1550		1550		1550		1550

		1600		1600		1600		1600		1600

		1650		1650		1650		1650		1650

		1700		1700		1700		1700		1700

		1750		1750		1750		1750		1750

		1800		1800		1800		1800		1800

		1850		1850		1850		1850		1850

		1900		1900		1900		1900		1900

		1950		1950		1950		1950		1950

		2000		2000		2000		2000		2000

		2050		2050		2050		2050		2050

		2100		2100		2100		2100		2100

		2150		2150		2150		2150		2150

		2200		2200		2200		2200		2200



R e d

O f f  W h I t e

M i s t  G r e e n

G a l  S t e e l

I N S U L T E C

Absorptance

1.078

0.729

1.146

0.96

1.038

1.153

0.916

1.053

0.349

1

1.19

1.103

1.09

0.312

1.038

1.178

1.115

1.072

0.286

1.038

1.115

0.75

0.692

0.268

0.417

1.072

0.156

0.66

0.249

0.112

1.121

0.156

0.623

0.237

0.087

1.109

0.137

0.517

0.231

0.087

0.81

0.118

0.611

0.249

0.076

0.685

0.125

0.579

0.262

0.0384

0.623

0.137

0.505

0.286

0.044

0.592

0.143

0.442

0.318

0.05

0.654

0.156

0.386

0.349

0.0384

0.698

0.181

0.38

0.343

0.05

0.598

0.206

0.361

0.349

0.012

0.592

0.087

0.318

0.349

0.075

0.193

0.118

0.193

0.386

0

0.287

0.224

0.243

0.349

0.075

0.386

0.349

0.324

0.33

0.187

0.5

0.474

0.405

0.33

0.299

0.598

0.654

0.5

0.343

0.384

0.741

0.76

0.604

0.324

0.48

0.879

0.704

0.673

0.324

0.474

0.685

0.866

0.66

0.305

0.349

0.729

0.766

0.692

0.305

0.499

0.729

0.75

0.71

0.293

0.424

0.704

0.75

0.692

0.286

0.467

0.735

0.75

0.72

0.274

0.449

0.804

0.766

0.692

0.268

0.48

0.76

0.729

0.698

0.262

0.461

0.773

0.75

0.71

0.243

0.48

0.754

0.75

0.72

0.243

0.461

0.729

0.723

0.692

0.237

0.46

0.748

0.723

0.698

0.231

0.486

0.704

0.679

0.654

0.231

0.486

0.729

0.704

0.673

0.224

0.46

0.729

0.704

0.654

0.231

0.495

0.698

0.679

0.648

0.218

0.48

0.735

0.717

0.679

0.224

0.474

0.735

0.723

0.692

0.237

0.495

0.735

0.723

0.704

0.243

0.474



Sheet1

				R e d		O f f  W h I t e		M i s t  G r e e n		G a l  S t e e l		I N S U L T E C

		0

		50

		100

		150

		200		1.078		0.729		1.146		0.96		1.038

		250		1.153		0.916		1.053		0.349		1

		300		1.19		1.103		1.09		0.312		1.038

		350		1.178		1.115		1.072		0.286		1.038

		400		1.115		0.75		0.692		0.268		0.417

		450		1.072		0.156		0.66		0.249		0.112

		500		1.121		0.156		0.623		0.237		0.087

		550		1.109		0.137		0.517		0.231		0.087

		600		0.81		0.118		0.611		0.249		0.076

		650		0.685		0.125		0.579		0.262		0.0384

		700		0.623		0.137		0.505		0.286		0.044

		750		0.592		0.143		0.442		0.318		0.05

		800		0.654		0.156		0.386		0.349		0.0384

		850		0.698		0.181		0.38		0.343		0.05

		900		0.598		0.206		0.361		0.349		0.012

		950		0.592		0.087		0.318		0.349		0.075

		1000		0.193		0.118		0.193		0.386		0

		1050		0.287		0.224		0.243		0.349		0.075

		1100		0.386		0.349		0.324		0.33		0.187

		1150		0.5		0.474		0.405		0.33		0.299

		1200		0.598		0.654		0.5		0.343		0.384

		1250		0.741		0.76		0.604		0.324		0.48

		1300		0.879		0.704		0.673		0.324		0.474

		1350		0.685		0.866		0.66		0.305		0.349

		1400		0.729		0.766		0.692		0.305		0.499

		1450		0.729		0.75		0.71		0.293		0.424

		1500		0.704		0.75		0.692		0.286		0.467

		1550		0.735		0.75		0.72		0.274		0.449

		1600		0.804		0.766		0.692		0.268		0.48

		1650		0.76		0.729		0.698		0.262		0.461

		1700		0.773		0.75		0.71		0.243		0.48

		1750		0.754		0.75		0.72		0.243		0.461

		1800		0.729		0.723		0.692		0.237		0.46

		1850		0.748		0.723		0.698		0.231		0.486

		1900		0.704		0.679		0.654		0.231		0.486

		1950		0.729		0.704		0.673		0.224		0.46

		2000		0.729		0.704		0.654		0.231		0.495

		2050		0.698		0.679		0.648		0.218		0.48

		2100		0.735		0.717		0.679		0.224		0.474

		2150		0.735		0.723		0.692		0.237		0.495

		2200		0.735		0.723		0.704		0.243		0.474





Sheet1

		0		0		0		0		0

		0		0		0		0		0

		0		0		0		0		0

		0		0		0		0		0

		0		0		0		0		0

		0		0		0		0		0

		0		0		0		0		0

		0		0		0		0		0

		0		0		0		0		0

		0		0		0		0		0

		0		0		0		0		0

		0		0		0		0		0

		0		0		0		0		0

		0		0		0		0		0

		0		0		0		0		0

		0		0		0		0		0

		0		0		0		0		0

		0		0		0		0		0

		0		0		0		0		0

		0		0		0		0		0

		0		0		0		0		0

		0		0		0		0		0

		0		0		0		0		0

		0		0		0		0		0

		0		0		0		0		0

		0		0		0		0		0

		0		0		0		0		0

		0		0		0		0		0

		0		0		0		0		0

		0		0		0		0		0

		0		0		0		0		0

		0		0		0		0		0

		0		0		0		0		0

		0		0		0		0		0

		0		0		0		0		0

		0		0		0		0		0

		0		0		0		0		0

		0		0		0		0		0

		0		0		0		0		0

		0		0		0		0		0

		0		0		0		0		0



0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0



Sheet2

		





Sheet3

		






_1099759801.xls
Chart4

		200

		250

		300

		350

		400

		450

		500

		550

		600

		650

		700

		750

		800

		850

		900

		950

		1000

		1050

		1100

		1150

		1200

		1250

		1300

		1350

		1400

		1450

		1500

		1550

		1600

		1650

		1700

		1750

		1800

		1850

		1900

		1950

		2000

		2050

		2100

		2150

		2200



Wavelength (nm)

Solar Radiation (W/m)

0

0

0

0.4

0.8

1.1

1.6

1.5

1.45

1.4

1.2

1.1

1

0.9

0.7

0.68

0.64

0.59

0.52

0.48

0.42

0.39

0.36

0

0

0.1

0.2

0.22

0.2

0.19

0.17

0.1

0

0

0

0.05

0.02

0.05

0.01

0



Sheet1

		wavelenght		sol rad

		200		0								x axis		sol rad W/m

		250		0										2

		300		0										1.8

		350		0.4										1.6

		400		0.8										1.4

		450		1.1										1.2

		500		1.6										1

		550		1.5										0.8

		600		1.45										0.6

		650		1.4										0.4

		700		1.2										0.2

		750		1.1										0

		800		1

		850		0.9

		900		0.7

		950		0.68

		1000		0.64

		1050		0.59

		1100		0.52

		1150		0.48

		1200		0.42

		1250		0.39

		1300		0.36

		1350		0

		1400		0

		1450		0.1

		1500		0.2

		1550		0.22

		1600		0.2

		1650		0.19

		1700		0.17

		1750		0.1

		1800		0

		1850		0

		1900		0

		1950		0.05

		2000		0.02

		2050		0.05

		2100		0.01

		2150		0

		2200





Sheet2

		





Sheet3

		






