[image: image1.png]



         .                                                                                                                                 .

E – A – B  Associates (Bayley-Edge Limited):

3 Craven Court, Craven Road, Altrincham, Cheshire, WA14 5DY England

Tel: (0)161 – 926 9077  Fax: (0) 161 – 927 7718   e-mail: ali@eabassoc.co.uk    http://www.eabassoc.co.uk
QUV Accelerated Weathering Test – August 1999

Aims

To test the durability of Solux radiation control coating Insultec 1.

Plates Tested

Plate 1:
Insultec on fibre cement board at coverage rate 2.5 m2/ltr. Primer CWS.

Plate 2:
Insultec on fibre cement board at coverage rate 2.5 m2/ltr. Primer CWS.

Plate 3:
Insultec on fibre cement board at coverage rate 2.5 m2/ltr. Primer CWS.

****************************************************************************************************

Method

Test Conditions:
4 hours at 640C.




4 hours humidity at 450C

Total Test Time:
Plate 1 removed at 2,010 QUV hours




Plate 2 removed at 1,048 QUV hours




Plate 3 removed at    743 QUV hours

****************************************************************************************************

Procedure

The plates were placed in the QUV machine at 32,752 hours and examined at 68, 743, 1048 and 2,010 QUV hours. Plate 3 was removed after 743 QUV hours, Plate 2 was removed after 1,048 QUV hours. Plate 1 was removed after 2,010 QUV hours.

****************************************************************************************************

Results

Inspection at 68 QUV hours

Plate 1:
No apparent change

Plate 2:
No apparent change

Plate 3:
No apparent change

Inspection at 743 QUV hours:
Plate 1:
A very slight colour change observed when plate held up to light. The coating had begun to loose its sheen and had become slightly matt in appearance.

Plate 2:
A very slight colour change observed when plate held up to light. The coating had begun to loose its sheen and had become slightly matt in appearance.

Plate 3:
A very slight colour change observed when plate held up to light. The coating had begun to loose its sheen and had become slightly matt in appearance. Removed from machine.

Plate 3 removed @ 33,495 hours (743 QUV hours)
Inspection at 1,048 QUV hours (equivalent to ( 5 years natural weathering):

Plate 1: 
Slight increase in the affect noted above.


Plate 2: 
Slight increase in the affect noted above.

Removed from machine

Plate 2 removed @ 33,800 hours (1,048 QUV hours).

Inspection at 2,010 QUV hours (equivalent to ( 10 years natural weathering):
Plate 1: 
Increase in the affect noted above. The coating had become whiter in colour and matt in appearance. Remove from machine.

Plate 1 removed @ 34,762 hours (2,010 QUV hours).
****************************************************************************************************

Conclusion

Insultec showed slight discolouration and lost of sheen.

Insultec performed very well and did not show any signs of failure in terms of durability.

****************************************************************************************************

