SPOORNET – FAX/FAKS

Telephone (012) 6719 362 fax number(012) 6719 351

Ref: S.RM (WE) 15/8/10/6/1/2

Date: 23rd September 1996

To fax number:  011 465 2381

Addressed to: Transvaal Metal Spraying Services



Attn: Mr. Alain De Comormond

From: 

V.I.T. Owner (Surface Protection)



Spoornet (Rolling Stock) CENTURIAN

INSULTEC, HEAT RETARDING COATING FOR PETROL TANK WAGONS.

We report back on your Insultec radiant heat barrier coating applied to the petrol tank wagons in January 1996.

The tank wagons convey petrol form the coastal depots at Port Elizabeth and East London to Upington in the Northern Cape Province, traveling a distance of approximately 1,000 kilometres.

The excessively high ambient temperatures attained while in transit and during the waiting time at Upington, before off loading, results in the petrol attaining a temperature in excess of 450C. These high temperatures result in evaporation and petrol loss.

The application of the Insultec system to the petrol tank wagons gave a considerable reduction in the temperature of the petrol (average of 100C). The test conducted were very satisfactory and twenty tank wagons will be coated with this system.

During the recent inspection of the tank wagons, it was noticed that the top coat has a tendency to retain dirt. To overcome this problem, we will be applying Insultec clear glaze as a final coat. It was interesting to note however that although the coating was covered with dirt and dust the tank body remained cool in direct sunlight.

We will carry out a series of test again during January 1997 and you will be kept informed.

Kind regards,

B.E Berner

V.I.T. OWNER (Surface Protection)

Hoofbestuurder (Rollende Materiaal)


General Manager (Rolling Stock)

Posbuz 30824





P.O. Box 30824

BRAAMFONTEIN




BRAAMFONTEIN

2017






2017

SPOORNET





SPOORNET

N Divisie Transnet Beprerk



A division of Transnet Limited

Registraslenommer 90/00900/06


Registration number 90 00900 

[image: image1.png]



Petrol Wagons: 10C cooler … less petrol lost

[image: image2.wmf]WAGON #38-500 418 (Upinton) - Graphite Grey - 

20

25

30

35

40

45

50

55

60

700

730

800

830

900

930

1000

1030

1100

1130

1200

1230

1300

1330

1400

1430

1500

1530

1600

1630

1700

1730

1800

1830

1900

1930

Time

Temperature C

PETROL

STEEL

AMBIENT


Petrol temperature is higher than ambient


[image: image3.wmf]WAGON # 38-505 541 (Upinton) - Aluminum -

20

25

30

35

40

45

50

55

60

700

730

800

830

900

930

1000

1030

1100

1130

1200

1230

1300

1330

1400

1430

1500

1530

1600

1630

1700

1730

1800

1830

1900

1930

Time

Temperature C

PETROL

STEEL

ALUM COAT

AMBIENT



 EMBED Excel.Chart.8 \s [image: image4.wmf]WAGON # 38-501 317 (Upington) - Insultec -

20

25

30

35

40

45

50

55

60

Time

Temperature C

PETROL

STEEL

INSULTEC

AMBIENT


Petrol temperature is lower than ambient
_1098254182.xls
Chart1

		700		700		700

		730		730		730

		800		800		800

		830		830		830

		900		900		900

		930		930		930

		1000		1000		1000

		1030		1030		1030

		1100		1100		1100

		1130		1130		1130

		1200		1200		1200

		1230		1230		1230

		1300		1300		1300

		1330		1330		1330

		1400		1400		1400

		1430		1430		1430

		1500		1500		1500

		1530		1530		1530

		1600		1600		1600

		1630		1630		1630

		1700		1700		1700

		1730		1730		1730

		1800		1800		1800

		1830		1830		1830

		1900		1900		1900

		1930		1930		1930



PETROL

STEEL

AMBIENT

Time

Temperature C

WAGON #38-500 418 (Upinton) - Graphite Grey -

30

25.7

23.4

29.6

25.6

24.1

29.6

26.9

24.7

29.7

28.2

26

29.8

30.1

26.7

30.2

30

29.6

30.9

36.5

29.5

32.5

43.9

29.9

34.1

45.7

31.3

35.5

48.7

33

35.7

50.5

33.6

36.2

53.5

34.4

37.5

54

34.7

38

54.7

35.7

39.1

56.6

36.7

40.3

58.2

36

41.5

57.4

36.6

42.4

58.4

35.4

43.5

57.4

37.1

44

55.1

38.1

44.3

52.5

38.2

44.5

50

38.2

44.3

47.1

30

41.1

44.5

32.5

42.8

42.2

31.3

42.4

39.4

29.7



Chart2

		700		700		700		700

		730		730		730		730

		800		800		800		800

		830		830		830		830

		900		900		900		900

		930		930		930		930

		1000		1000		1000		1000

		1030		1030		1030		1030

		1100		1100		1100		1100

		1130		1130		1130		1130

		1200		1200		1200		1200

		1230		1230		1230		1230

		1300		1300		1300		1300

		1330		1330		1330		1330

		1400		1400		1400		1400

		1430		1430		1430		1430

		1500		1500		1500		1500

		1530		1530		1530		1530

		1600		1600		1600		1600

		1630		1630		1630		1630

		1700		1700		1700		1700

		1730		1730		1730		1730

		1800		1800		1800		1800

		1830		1830		1830		1830

		1900		1900		1900		1900

		1930		1930		1930		1930



PETROL

STEEL

ALUM COAT

AMBIENT

Time

Temperature C

WAGON # 38-505 541 (Upinton) - Aluminum -

29.5

25.8

25

23.4

29.3

25.7

25.4

24.1

28.9

26.5

26.5

24.7

29

27.5

27.4

26

29.1

28.3

28.7

26.7

29.1

30.1

33

29.6

29.2

33.5

36.4

29.5

30.5

36

38.1

29.9

32.1

38.9

42.8

31.3

33.4

43.1

45.6

33

34.1

44.6

46.8

33.6

34.7

46.6

48.1

34.4

36

49.1

50.5

34.7

36.2

49.3

48.2

35.7

36.9

51.1

52

36.7

38.5

52.3

52.6

36

39.6

51.4

51.8

36.6

41.9

52.3

52.4

35.4

42

52.7

50.6

37.1

42.2

53.2

53.8

36.1

42.5

52

50.5

38.2

42.8

48.6

47.8

38.2

42.6

44.7

43.6

33

42.2

42.7

41.5

32.5

41.9

41.5

41.5

31.3

41.5

39

39

29.7



Chart3

		700		700		700		700

		730		730		730		730

		800		800		800		800

		830		830		830		830

		900		900		900		900

		930		930		930		930

		1000		1000		1000		1000

		1030		1030		1030		1030

		1100		1100		1100		1100

		1130		1130		1130		1130

		1200		1200		1200		1200

		1230		1230		1230		1230

		1300		1300		1300		1300

		1330		1330		1330		1330

		1400		1400		1400		1400

		1430		1430		1430		1430

		1500		1500		1500		1500

		1530		1530		1530		1530

		1600		1600		1600		1600

		1630		1630		1630		1630

		1700		1700		1700		1700

		1730		1730		1730		1730

		1800		1800		1800		1800

		1830		1830		1830		1830

		1900		1900		1900		1900

		1930		1930		1930		1930



PETROL

STEEL

COATING

AMBIENT

Time

Temperature C

WAGON #38-501 317 (Upington) - Insultec -

27.8

24.7

24.2

23.4

27.7

24.9

24.6

24.1

27.6

25.1

26.5

24.7

27.5

27.4

27.5

26

27.4

28.8

26.7

26.7

27.5

31.1

31.9

29.6

27.7

33.1

33

29.5

26.2

35.5

33.4

29.9

28.6

37.4

37.2

31.3

29.2

38.6

38.7

33

29.6

39.6

40

33.5

30

41

42

34.4

30.4

41.5

42

34.7

31.6

41.8

43.3

35.7

32.3

42.1

43.4

36.7

32.9

42.7

44.3

36

33.4

42.6

44.8

36.6

34

42.5

43.5

35.4

34.4

40.8

41.6

37.1

34.8

39.4

38.2

38.1

35.3

39.6

36.6

38.2

35.7

39.8

36.8

38.2

35.5

36

36.6

33.3

35.3

34.2

34.4

32.5

35

34.3

32.5

31.3

34.7

31.4

30.9

29.7



Sheet1

				WAGON # 38-500 415 (UPINGTON)										WAGON # 38-505 541 (UPINGTON)												WAGON # 38-501 317 (UPINGTON)

						Graphite Grey (chart 1)										Aluminum (chart 2)												Insultec (chart 3)

				PETROL		STEEL		AMBIENT						PETROL		STEEL		ALUM COAT		AMBIENT						PETROL		STEEL		COATING		AMBIENT

		700		30		25.7		23.4				700		29.5		25.8		25		23.4				700		27.8		24.7		24.2		23.4

		730		29.6		25.6		24.1				730		29.3		25.7		25.4		24.1				730		27.7		24.9		24.6		24.1

		800		29.6		26.9		24.7				800		28.9		26.5		26.5		24.7				800		27.6		25.1		26.5		24.7

		830		29.7		28.2		26				830		29		27.5		27.4		26				830		27.5		27.4		27.5		26

		900		29.8		30.1		26.7				900		29.1		28.3		28.7		26.7				900		27.4		28.8		26.7		26.7

		930		30.2		30		29.6				930		29.1		30.1		33		29.6				930		27.5		31.1		31.9		29.6

		1000		30.9		36.5		29.5				1000		29.2		33.5		36.4		29.5				1000		27.7		33.1		33		29.5

		1030		32.5		43.9		29.9				1030		30.5		36		38.1		29.9				1030		26.2		35.5		33.4		29.9

		1100		34.1		45.7		31.3				1100		32.1		38.9		42.8		31.3				1100		28.6		37.4		37.2		31.3

		1130		35.5		48.7		33				1130		33.4		43.1		45.6		33				1130		29.2		38.6		38.7		33

		1200		35.7		50.5		33.6				1200		34.1		44.6		46.8		33.6				1200		29.6		39.6		40		33.5

		1230		36.2		53.5		34.4				1230		34.7		46.6		48.1		34.4				1230		30		41		42		34.4

		1300		37.5		54		34.7				1300		36		49.1		50.5		34.7				1300		30.4		41.5		42		34.7

		1330		38		54.7		35.7				1330		36.2		49.3		48.2		35.7				1330		31.6		41.8		43.3		35.7

		1400		39.1		56.6		36.7				1400		36.9		51.1		52		36.7				1400		32.3		42.1		43.4		36.7

		1430		40.3		58.2		36				1430		38.5		52.3		52.6		36				1430		32.9		42.7		44.3		36

		1500		41.5		57.4		36.6				1500		39.6		51.4		51.8		36.6				1500		33.4		42.6		44.8		36.6

		1530		42.4		58.4		35.4				1530		41.9		52.3		52.4		35.4				1530		34		42.5		43.5		35.4

		1600		43.5		57.4		37.1				1600		42		52.7		50.6		37.1				1600		34.4		40.8		41.6		37.1

		1630		44		55.1		38.1				1630		42.2		53.2		53.8		36.1				1630		34.8		39.4		38.2		38.1

		1700		44.3		52.5		38.2				1700		42.5		52		50.5		38.2				1700		35.3		39.6		36.6		38.2

		1730		44.5		50		38.2				1730		42.8		48.6		47.8		38.2				1730		35.7		39.8		36.8		38.2

		1800		44.3		47.1		30				1800		42.6		44.7		43.6		33				1800		35.5		36		36.6		33.3

		1830		41.1		44.5		32.5				1830		42.2		42.7		41.5		32.5				1830		35.3		34.2		34.4		32.5

		1900		42.8		42.2		31.3				1900		41.9		41.5		41.5		31.3				1900		35		34.3		32.5		31.3

		1930		42.4		39.4		29.7				1930		41.5		39		39		29.7				1930		34.7		31.4		30.9		29.7





Sheet2

		





Sheet3

		






_1098254361.xls
Chart1

		700		700		700

		730		730		730

		800		800		800

		830		830		830

		900		900		900

		930		930		930

		1000		1000		1000

		1030		1030		1030

		1100		1100		1100

		1130		1130		1130

		1200		1200		1200

		1230		1230		1230

		1300		1300		1300

		1330		1330		1330

		1400		1400		1400

		1430		1430		1430

		1500		1500		1500

		1530		1530		1530

		1600		1600		1600

		1630		1630		1630

		1700		1700		1700

		1730		1730		1730

		1800		1800		1800

		1830		1830		1830

		1900		1900		1900

		1930		1930		1930



PETROL

STEEL

AMBIENT

Time

Temperature C

WAGON #38-500 418 (Upinton) - Graphite Grey -

30

25.7

23.4

29.6

25.6

24.1

29.6

26.9

24.7

29.7

28.2

26

29.8

30.1

26.7

30.2

30

29.6

30.9

36.5

29.5

32.5

43.9

29.9

34.1

45.7

31.3

35.5

48.7

33

35.7

50.5

33.6

36.2

53.5

34.4

37.5

54

34.7

38

54.7

35.7

39.1

56.6

36.7

40.3

58.2

36

41.5

57.4

36.6

42.4

58.4

35.4

43.5

57.4

37.1

44

55.1

38.1

44.3

52.5

38.2

44.5

50

38.2

44.3

47.1

30

41.1

44.5

32.5

42.8

42.2

31.3

42.4

39.4

29.7



Chart2

		700		700		700		700

		730		730		730		730

		800		800		800		800

		830		830		830		830

		900		900		900		900

		930		930		930		930

		1000		1000		1000		1000

		1030		1030		1030		1030

		1100		1100		1100		1100

		1130		1130		1130		1130

		1200		1200		1200		1200

		1230		1230		1230		1230

		1300		1300		1300		1300

		1330		1330		1330		1330

		1400		1400		1400		1400

		1430		1430		1430		1430

		1500		1500		1500		1500

		1530		1530		1530		1530

		1600		1600		1600		1600

		1630		1630		1630		1630

		1700		1700		1700		1700

		1730		1730		1730		1730

		1800		1800		1800		1800

		1830		1830		1830		1830

		1900		1900		1900		1900

		1930		1930		1930		1930



PETROL

STEEL

coating

AMBIENT

Time

Temperature C

WAGON # 38-505 541 (Upinton) - Aluminum -

29.5

25.8

25

23.4

29.3

25.7

25.4

24.1

28.9

26.5

26.5

24.7

29

27.5

27.4

26

29.1

28.3

28.7

26.7

29.1

30.1

33

29.6

29.2

33.5

36.4

29.5

30.5

36

38.1

29.9

32.1

38.9

42.8

31.3

33.4

43.1

45.6

33

34.1

44.6

46.8

33.6

34.7

46.6

48.1

34.4

36

49.1

50.5

34.7

36.2

49.3

48.2

35.7

36.9

51.1

52

36.7

38.5

52.3

52.6

36

39.6

51.4

51.8

36.6

41.9

52.3

52.4

35.4

42

52.7

50.6

37.1

42.2

53.2

53.8

36.1

42.5

52

50.5

38.2

42.8

48.6

47.8

38.2

42.6

44.7

43.6

33

42.2

42.7

41.5

32.5

41.9

41.5

41.5

31.3

41.5

39

39

29.7



Chart3

		700		700		700		700

		730		730		730		730

		800		800		800		800

		830		830		830		830

		900		900		900		900

		930		930		930		930

		1000		1000		1000		1000

		1030		1030		1030		1030

		1100		1100		1100		1100

		1130		1130		1130		1130

		1200		1200		1200		1200

		1230		1230		1230		1230

		1300		1300		1300		1300

		1330		1330		1330		1330

		1400		1400		1400		1400

		1430		1430		1430		1430

		1500		1500		1500		1500

		1530		1530		1530		1530

		1600		1600		1600		1600

		1630		1630		1630		1630

		1700		1700		1700		1700

		1730		1730		1730		1730

		1800		1800		1800		1800

		1830		1830		1830		1830

		1900		1900		1900		1900

		1930		1930		1930		1930



PETROL

STEEL

INSULTEC

AMBIENT

Time

Temperature C

WAGON #38-501 317 (Upington) - Insultec -

27.8

24.7

24.2

23.4

27.7

24.9

24.6

24.1

27.6

25.1

26.5

24.7

27.5

27.4

27.5

26

27.4

28.8

26.7

26.7

27.5

31.1

31.9

29.6

27.7

33.1

33

29.5

26.2

35.5

33.4

29.9

28.6

37.4

37.2

31.3

29.2

38.6

38.7

33

29.6

39.6

40

33.5

30

41

42

34.4

30.4

41.5

42

34.7

31.6

41.8

43.3

35.7

32.3

42.1

43.4

36.7

32.9

42.7

44.3

36

33.4

42.6

44.8

36.6

34

42.5

43.5

35.4

34.4

40.8

41.6

37.1

34.8

39.4

38.2

38.1

35.3

39.6

36.6

38.2

35.7

39.8

36.8

38.2

35.5

36

36.6

33.3

35.3

34.2

34.4

32.5

35

34.3

32.5

31.3

34.7

31.4

30.9

29.7



Chart4

		700		700		700		700

		730		730		730		730

		800		800		800		800

		830		830		830		830

		900		900		900		900

		930		930		930		930

		1000		1000		1000		1000

		1030		1030		1030		1030

		1100		1100		1100		1100

		1130		1130		1130		1130

		1200		1200		1200		1200

		1230		1230		1230		1230

		1300		1300		1300		1300

		1330		1330		1330		1330

		1400		1400		1400		1400

		1430		1430		1430		1430

		1500		1500		1500		1500

		1530		1530		1530		1530

		1600		1600		1600		1600

		1630		1630		1630		1630

		1700		1700		1700		1700

		1730		1730		1730		1730

		1800		1800		1800		1800

		1830		1830		1830		1830

		1900		1900		1900		1900

		1930		1930		1930		1930



PETROL

STEEL

INSULTEC

AMBIENT

Time

Temperature C

WAGON # 38-501 317 (Upington) - Insultec -

27.8

24.7

24.2

23.4

27.7

24.9

24.6

24.1

27.6

25.1

26.5

24.7

27.5

27.4

27.5

26

27.4

28.8

26.7

26.7

27.5

31.1

31.9

29.6

27.7

33.1

33

29.5

26.2

35.5

33.4

29.9

28.6

37.4

37.2

31.3

29.2

38.6

38.7

33

29.6

39.6

40

33.5

30

41

42

34.4

30.4

41.5

42

34.7

31.6

41.8

43.3

35.7

32.3

42.1

43.4

36.7

32.9

42.7

44.3

36

33.4

42.6

44.8

36.6

34

42.5

43.5

35.4

34.4

40.8

41.6

37.1

34.8

39.4

38.2

38.1

35.3

39.6

36.6

38.2

35.7

39.8

36.8

38.2

35.5

36

36.6

33.3

35.3

34.2

34.4

32.5

35

34.3

32.5

31.3

34.7

31.4

30.9

29.7



Sheet1

				WAGON # 38-500 415 (UPINGTON)										WAGON # 38-505 541 (UPINGTON)												WAGON # 38-501 317 (UPINGTON)

						Graphite Grey (chart 1)										Aluminum (chart 2)												Insultec (chart 3)

				PETROL		STEEL		AMBIENT						PETROL		STEEL		coating		AMBIENT						PETROL		STEEL		INSULTEC		AMBIENT

		700		30		25.7		23.4				700		29.5		25.8		25		23.4				700		27.8		24.7		24.2		23.4

		730		29.6		25.6		24.1				730		29.3		25.7		25.4		24.1				730		27.7		24.9		24.6		24.1

		800		29.6		26.9		24.7				800		28.9		26.5		26.5		24.7				800		27.6		25.1		26.5		24.7

		830		29.7		28.2		26				830		29		27.5		27.4		26				830		27.5		27.4		27.5		26

		900		29.8		30.1		26.7				900		29.1		28.3		28.7		26.7				900		27.4		28.8		26.7		26.7

		930		30.2		30		29.6				930		29.1		30.1		33		29.6				930		27.5		31.1		31.9		29.6

		1000		30.9		36.5		29.5				1000		29.2		33.5		36.4		29.5				1000		27.7		33.1		33		29.5

		1030		32.5		43.9		29.9				1030		30.5		36		38.1		29.9				1030		26.2		35.5		33.4		29.9

		1100		34.1		45.7		31.3				1100		32.1		38.9		42.8		31.3				1100		28.6		37.4		37.2		31.3

		1130		35.5		48.7		33				1130		33.4		43.1		45.6		33				1130		29.2		38.6		38.7		33

		1200		35.7		50.5		33.6				1200		34.1		44.6		46.8		33.6				1200		29.6		39.6		40		33.5

		1230		36.2		53.5		34.4				1230		34.7		46.6		48.1		34.4				1230		30		41		42		34.4

		1300		37.5		54		34.7				1300		36		49.1		50.5		34.7				1300		30.4		41.5		42		34.7

		1330		38		54.7		35.7				1330		36.2		49.3		48.2		35.7				1330		31.6		41.8		43.3		35.7

		1400		39.1		56.6		36.7				1400		36.9		51.1		52		36.7				1400		32.3		42.1		43.4		36.7

		1430		40.3		58.2		36				1430		38.5		52.3		52.6		36				1430		32.9		42.7		44.3		36

		1500		41.5		57.4		36.6				1500		39.6		51.4		51.8		36.6				1500		33.4		42.6		44.8		36.6

		1530		42.4		58.4		35.4				1530		41.9		52.3		52.4		35.4				1530		34		42.5		43.5		35.4

		1600		43.5		57.4		37.1				1600		42		52.7		50.6		37.1				1600		34.4		40.8		41.6		37.1

		1630		44		55.1		38.1				1630		42.2		53.2		53.8		36.1				1630		34.8		39.4		38.2		38.1

		1700		44.3		52.5		38.2				1700		42.5		52		50.5		38.2				1700		35.3		39.6		36.6		38.2

		1730		44.5		50		38.2				1730		42.8		48.6		47.8		38.2				1730		35.7		39.8		36.8		38.2

		1800		44.3		47.1		30				1800		42.6		44.7		43.6		33				1800		35.5		36		36.6		33.3

		1830		41.1		44.5		32.5				1830		42.2		42.7		41.5		32.5				1830		35.3		34.2		34.4		32.5

		1900		42.8		42.2		31.3				1900		41.9		41.5		41.5		31.3				1900		35		34.3		32.5		31.3

		1930		42.4		39.4		29.7				1930		41.5		39		39		29.7				1930		34.7		31.4		30.9		29.7





Sheet2

		





Sheet3

		






_1097610107.xls
Chart1

		700		700		700

		730		730		730

		800		800		800

		830		830		830

		900		900		900

		930		930		930

		1000		1000		1000

		1030		1030		1030

		1100		1100		1100

		1130		1130		1130

		1200		1200		1200

		1230		1230		1230

		1300		1300		1300

		1330		1330		1330

		1400		1400		1400

		1430		1430		1430

		1500		1500		1500

		1530		1530		1530

		1600		1600		1600

		1630		1630		1630

		1700		1700		1700

		1730		1730		1730

		1800		1800		1800

		1830		1830		1830

		1900		1900		1900

		1930		1930		1930



PETROL

STEEL

AMBIENT

Time

Temperature C

WAGON #38-500 418 (Upinton) - Graphite Grey -

30

25.7

23.4

29.6

25.6

24.1

29.6

26.9

24.7

29.7

28.2

26

29.8

30.1

26.7

30.2

30

29.6

30.9

36.5

29.5

32.5

43.9

29.9

34.1

45.7

31.3

35.5

48.7

33

35.7

50.5

33.6

36.2

53.5

34.4

37.5

54

34.7

38

54.7

35.7

39.1

56.6

36.7

40.3

58.2

36

41.5

57.4

36.6

42.4

58.4

35.4

43.5

57.4

37.1

44

55.1

38.1

44.3

52.5

38.2

44.5

50

38.2

44.3

47.1

30

41.1

44.5

32.5

42.8

42.2

31.3

42.4

39.4

29.7



Chart2

		700		700		700		700

		730		730		730		730

		800		800		800		800

		830		830		830		830

		900		900		900		900

		930		930		930		930

		1000		1000		1000		1000

		1030		1030		1030		1030

		1100		1100		1100		1100

		1130		1130		1130		1130

		1200		1200		1200		1200

		1230		1230		1230		1230

		1300		1300		1300		1300

		1330		1330		1330		1330

		1400		1400		1400		1400

		1430		1430		1430		1430

		1500		1500		1500		1500

		1530		1530		1530		1530

		1600		1600		1600		1600

		1630		1630		1630		1630

		1700		1700		1700		1700

		1730		1730		1730		1730

		1800		1800		1800		1800

		1830		1830		1830		1830

		1900		1900		1900		1900

		1930		1930		1930		1930



PETROL

STEEL

coating

AMBIENT

Time

Temperature C

WAGON # 38-505 541 (Upinton) - Aluminum -

29.5

25.8

25

23.4

29.3

25.7

25.4

24.1

28.9

26.5

26.5

24.7

29

27.5

27.4

26

29.1

28.3

28.7

26.7

29.1

30.1

33

29.6

29.2

33.5

36.4

29.5

30.5

36

38.1

29.9

32.1

38.9

42.8

31.3

33.4

43.1

45.6

33

34.1

44.6

46.8

33.6

34.7

46.6

48.1

34.4

36

49.1

50.5

34.7

36.2

49.3

48.2

35.7

36.9

51.1

52

36.7

38.5

52.3

52.6

36

39.6

51.4

51.8

36.6

41.9

52.3

52.4

35.4

42

52.7

50.6

37.1

42.2

53.2

53.8

36.1

42.5

52

50.5

38.2

42.8

48.6

47.8

38.2

42.6

44.7

43.6

33

42.2

42.7

41.5

32.5

41.9

41.5

41.5

31.3

41.5

39

39

29.7



Chart3

		700		700		700		700

		730		730		730		730

		800		800		800		800

		830		830		830		830

		900		900		900		900

		930		930		930		930

		1000		1000		1000		1000

		1030		1030		1030		1030

		1100		1100		1100		1100

		1130		1130		1130		1130

		1200		1200		1200		1200

		1230		1230		1230		1230

		1300		1300		1300		1300

		1330		1330		1330		1330

		1400		1400		1400		1400

		1430		1430		1430		1430

		1500		1500		1500		1500

		1530		1530		1530		1530

		1600		1600		1600		1600

		1630		1630		1630		1630

		1700		1700		1700		1700

		1730		1730		1730		1730

		1800		1800		1800		1800

		1830		1830		1830		1830

		1900		1900		1900		1900

		1930		1930		1930		1930



PETROL

STEEL

COATING

AMBIENT

Time

Temperature C

WAGON #38-501 317 (Upington) - Insultec -

27.8

24.7

24.2

23.4

27.7

24.9

24.6

24.1

27.6

25.1

26.5

24.7

27.5

27.4

27.5

26

27.4

28.8

26.7

26.7

27.5

31.1

31.9

29.6

27.7

33.1

33

29.5

26.2

35.5

33.4

29.9

28.6

37.4

37.2

31.3

29.2

38.6

38.7

33

29.6

39.6

40

33.5

30

41

42

34.4

30.4

41.5

42

34.7

31.6

41.8

43.3

35.7

32.3

42.1

43.4

36.7

32.9

42.7

44.3

36

33.4

42.6

44.8

36.6

34

42.5

43.5

35.4

34.4

40.8

41.6

37.1

34.8

39.4

38.2

38.1

35.3

39.6

36.6

38.2

35.7

39.8

36.8

38.2

35.5

36

36.6

33.3

35.3

34.2

34.4

32.5

35

34.3

32.5

31.3

34.7

31.4

30.9

29.7



Chart4

		700		700		700		700

		730		730		730		730

		800		800		800		800

		830		830		830		830

		900		900		900		900

		930		930		930		930

		1000		1000		1000		1000

		1030		1030		1030		1030

		1100		1100		1100		1100

		1130		1130		1130		1130

		1200		1200		1200		1200

		1230		1230		1230		1230

		1300		1300		1300		1300

		1330		1330		1330		1330

		1400		1400		1400		1400

		1430		1430		1430		1430

		1500		1500		1500		1500

		1530		1530		1530		1530

		1600		1600		1600		1600

		1630		1630		1630		1630

		1700		1700		1700		1700

		1730		1730		1730		1730

		1800		1800		1800		1800

		1830		1830		1830		1830

		1900		1900		1900		1900

		1930		1930		1930		1930



PETROL

STEEL

COATING

AMBIENT

Time

Temperature C

WAGON # 38-501 317 (Upington) - Insultec -

27.8

24.7

24.2

23.4

27.7

24.9

24.6

24.1

27.6

25.1

26.5

24.7

27.5

27.4

27.5

26

27.4

28.8

26.7

26.7

27.5

31.1

31.9

29.6

27.7

33.1

33

29.5

26.2

35.5

33.4

29.9

28.6

37.4

37.2

31.3

29.2

38.6

38.7

33

29.6

39.6

40

33.5

30

41

42

34.4

30.4

41.5

42

34.7

31.6

41.8

43.3

35.7

32.3

42.1

43.4

36.7

32.9

42.7

44.3

36

33.4

42.6

44.8

36.6

34

42.5

43.5

35.4

34.4

40.8

41.6

37.1

34.8

39.4

38.2

38.1

35.3

39.6

36.6

38.2

35.7

39.8

36.8

38.2

35.5

36

36.6

33.3

35.3

34.2

34.4

32.5

35

34.3

32.5

31.3

34.7

31.4

30.9

29.7



Sheet1

				WAGON # 38-500 415 (UPINGTON)										WAGON # 38-505 541 (UPINGTON)												WAGON # 38-501 317 (UPINGTON)

						Graphite Grey (chart 1)										Aluminum (chart 2)												Insultec (chart 3)

				PETROL		STEEL		AMBIENT						PETROL		STEEL		coating		AMBIENT						PETROL		STEEL		COATING		AMBIENT

		700		30		25.7		23.4				700		29.5		25.8		25		23.4				700		27.8		24.7		24.2		23.4

		730		29.6		25.6		24.1				730		29.3		25.7		25.4		24.1				730		27.7		24.9		24.6		24.1

		800		29.6		26.9		24.7				800		28.9		26.5		26.5		24.7				800		27.6		25.1		26.5		24.7

		830		29.7		28.2		26				830		29		27.5		27.4		26				830		27.5		27.4		27.5		26

		900		29.8		30.1		26.7				900		29.1		28.3		28.7		26.7				900		27.4		28.8		26.7		26.7

		930		30.2		30		29.6				930		29.1		30.1		33		29.6				930		27.5		31.1		31.9		29.6

		1000		30.9		36.5		29.5				1000		29.2		33.5		36.4		29.5				1000		27.7		33.1		33		29.5

		1030		32.5		43.9		29.9				1030		30.5		36		38.1		29.9				1030		26.2		35.5		33.4		29.9

		1100		34.1		45.7		31.3				1100		32.1		38.9		42.8		31.3				1100		28.6		37.4		37.2		31.3

		1130		35.5		48.7		33				1130		33.4		43.1		45.6		33				1130		29.2		38.6		38.7		33

		1200		35.7		50.5		33.6				1200		34.1		44.6		46.8		33.6				1200		29.6		39.6		40		33.5

		1230		36.2		53.5		34.4				1230		34.7		46.6		48.1		34.4				1230		30		41		42		34.4

		1300		37.5		54		34.7				1300		36		49.1		50.5		34.7				1300		30.4		41.5		42		34.7

		1330		38		54.7		35.7				1330		36.2		49.3		48.2		35.7				1330		31.6		41.8		43.3		35.7

		1400		39.1		56.6		36.7				1400		36.9		51.1		52		36.7				1400		32.3		42.1		43.4		36.7

		1430		40.3		58.2		36				1430		38.5		52.3		52.6		36				1430		32.9		42.7		44.3		36

		1500		41.5		57.4		36.6				1500		39.6		51.4		51.8		36.6				1500		33.4		42.6		44.8		36.6

		1530		42.4		58.4		35.4				1530		41.9		52.3		52.4		35.4				1530		34		42.5		43.5		35.4

		1600		43.5		57.4		37.1				1600		42		52.7		50.6		37.1				1600		34.4		40.8		41.6		37.1

		1630		44		55.1		38.1				1630		42.2		53.2		53.8		36.1				1630		34.8		39.4		38.2		38.1

		1700		44.3		52.5		38.2				1700		42.5		52		50.5		38.2				1700		35.3		39.6		36.6		38.2

		1730		44.5		50		38.2				1730		42.8		48.6		47.8		38.2				1730		35.7		39.8		36.8		38.2

		1800		44.3		47.1		30				1800		42.6		44.7		43.6		33				1800		35.5		36		36.6		33.3

		1830		41.1		44.5		32.5				1830		42.2		42.7		41.5		32.5				1830		35.3		34.2		34.4		32.5

		1900		42.8		42.2		31.3				1900		41.9		41.5		41.5		31.3				1900		35		34.3		32.5		31.3

		1930		42.4		39.4		29.7				1930		41.5		39		39		29.7				1930		34.7		31.4		30.9		29.7





Sheet2

		





Sheet3

		






